## Slide 1
Petar V Peshev
Time-Domain Lab
EE4730 High Frequency Wireless
Architectures

## Slide 2: Table of Contents
    Time-Domain Setup & Equipment
    Methodology
    Beam-Path Alignment
    Dielectric Characterization
        Permittivity
        Loss Tangent & Attenuation Constant
    Appendices
30-07-2023

## Slide 3: Time-Domain Spectroscopy Setup
    Pump pulse generation
        Pulsed laser, 800nm
        Beam splitter
    Optical fibers
    Optical delay
    THz beam-path
        TX & RX PCA
        Plano-convex lenses
    Electronics
        DC source
        LNA
        ADC
30-07-2023

## Slide 4: Pulsed Laser
    Generates laser pulses (instead of continuous
    laser signal)
    Pulse repetition rate
    Emitted energy has Gaussian spatial distribution
    Pulses are equal and repetitive; hence, average
    emitted laser power
30-07-2023

## Slide 5: Optical Delay
    Consists of moving mirrors
    Introduces delay into gating pulse of RX PCA
    Laser / gating pulse increases conductivity of
    the RX PCA for a certain time (defined by )
    To sample the THz electric field, the peak
    conductivity must be moved in time over the time
    range
    Achieved using multiple excitations over different
30-07-2023

## Slide 6: Photoconductive Antenna
    Laser pulses moves electrons from valence
    to conduction band (increase conductivity)
    TX PCA
    PCA is biased
    Freed electrons start to move across the gap
    and create THz field
    RX PCA
    THz field is incident on the PCA
    Freed electrons move across the gap due to
    THz field and cause current flow
30-07-2023

## Slide 7: Electronics
    Excitation and induced current at RX PCA terminals
    happens faster than sampling rate of ADC
    The ADC samples the average induced voltage
    over many samples
    Signal-to-Noise ratio is related to the integration time
    Larger integration time, smaller noise (larger ),
    but slower sampling
30-07-2023

## Slide 8: Plano-Convex Lenses
    Four similar plano-convex lenses with focal
    length mm
    THz beam is collimated between first-second
    and third-fourth lenses, and focused between
    second-third
30-07-2023

## Slide 9: Methodology
    1. Choose number of averaged samples to
    increase SNR
    2. Align THz beam-path (PCAs and lenses) to
    increase the power of the received reference
    signal (no sample)
    3. Record reference and sample signal
    (reference, samples A / B / C)
    4. Use time-delay between recorded reference
    and sample pulses to derive sample permittivity
    5. Use frequency domain ratio between reference
    and sample to derive attenuation constant and
    loss tangent with TL model
30-07-2023

## Slide 10: Number of Averaged Samples
    Averaging more samples
    Reduces noise (increases )
    Increases measurement acquisition time
    Number of averaged samples,
    samples
    dB
30-07-2023

## Slide 11: Terahertz Beam-Path Alignment
    Goal: maximize the reference signal amplitude (achieved V)
    Plano-convex lens:
        TPX50
        mm
30-07-2023

## Slide 12: Calibrated Reference Signal
30-07-2023
    Useful band up to 2.0 – 2.5 THz

## Slide 13: Characterization: Permittivity
    Wave propagation through sample is slower
    Use pulse delay between reference and sample
    signals to estimate the speed of light inside the
    dielectric and permittivity
30-07-2023

## Slide 14: Sample Signals
30-07-2023

## Slide 15: Characterization: Loss Tangent and Attenuation Constant (1)
    Small losses in good dielectric approximation (Advanced EM)
    , where
    The ratio between input and output forward propagating waves
    for each frequency is derived from the ratio between the
    signals’ frequency domain
    Convert measurements to frequency domain
    Calculate ratio between frequency domain
    signals
30-07-2023

## Slide 16: Characterization: Loss Tangent and Attenuation Constant (2)
    Use TL model ratio between input and output
    forward propagating waves
        Calculate ratio for an array of different
        values
        Choose loss tangent with smallest absolute
        value difference between measurements and
        TL model calculation
30-07-2023

## Slide 17: Loss Tangent and Attenuation Constant: Silicon (Sample A)
30-07-2023
    Highest losses

## Slide 18: Loss Tangent and Attenuation Constant: Gore-Tex (Sample B)
30-07-2023
    Second highest losses

## Slide 19: Loss Tangent and Attenuation Constant: Teflon (Sample C)
30-07-2023
    Least losses

## Slide 20: Power Spectral Density: Silicon (Sample A)
30-07-2023

## Slide 21: Power Spectral Density: Gore-Tex (Sample B)
30-07-2023

## Slide 22: Power Spectral Density: Teflon (Sample C)
30-07-2023

## Slide 23: Q & A

## Slide 24: Thank you for your attention
Petar V Peshev

## Slide 25: Appendices

## Slide 26: Appendix A: Transmission Line Model
    and
    (wave is continuous across interface)
    (wave is continuous across interface)
30-07-2023

## Slide 27: Appendix B: Photoconductive Antenna Model
    Increasing optical power, increases impressed current
    and decreases Norton impedance
30-07-2023

## Slide 28: Appendix C: Time-Gated Signals (1)
30-07-2023
    Time-gating can be used to remove noise and reflections

## Slide 29: Appendix C: Time-Gated Signals (2)
30-07-2023

## Slide 30: Appendix C: Time-Gated Signals (3)
30-07-2023

## Slide 31: Appendix C: Time-Gated Signals (4)
30-07-2023

## Slide 32: Appendix C: Time-Gated Signals (5)
30-07-2023

## Slide 33: Appendix C: Time-Gated Signals (6)
30-07-2023

## Slide 34: Appendix C: Time-Gated Signals (7)
30-07-2023

## Slide 35: Appendix C: Time-Gated Signals (8)
30-07-2023